The General Chemical Resistance of Various Elastomers

This chart is offered only as a general guide, indicating the suitability of various elastomers for service in these chemicals and fluids. The ratings are based for the most part, on published literature of various polymer suppliers, rubber manufacturers, and in some cases, the considered opinion of experienced compounders. We cannot guarantee their accuracy nor assume the responsibility for use thereof. Many factors must be considered in using a rubber part in service. The most important as we see them are:

- Temperature of service: Higher temperatures increase the effect of all chemicals on polymers. The increase varies with the polymer and the chemical. a compound quite suitable at room temperature might fail miserably at elevated temperature.

- Conditions of Service: A compound that swells badly might still function well as a static seal yet fail in any dynamic application.

- The Grade of the Polymer: Many types of polymers are available in different grades that vary greatly in chemical resistance.

- The Compound itself: compounds designed for other outstanding properties may be poorer in performance in a chemical than one designed especially for fluid resistance.

- The Durometer: In general, the harder a compound the better its resistance.

In light of the above factors, its always best to test.

General Purpose - Non Oil Resistant

| FLUID CHART KEY | (1) | (2) | (3) | (4) |
| --- | --- | --- | --- | --- |
| TYPE OF | Natural Rub- | Butadiene | Butyl | Ethylene Pro- |
| RUBBER | ber NR | Styrene |  | pylene EPM |
|  |  | SBR |  |  |
| Material and | Isoprene | Butadiene | IIR | EPDM |
| ASTM Desig- |  |  |  |  |
| nation |  |  |  |  |
| CHEMICAL | Poly | Poly Butadi- | Isobutylene | Ethylene |
| GROUP | Isoprene | ene | Isoprene | Propylene Co- |
|  |  | Butadiene | Polymer | polymer and |
|  |  | Styrene |  | Terpolymer |
|  |  | Copolymer |  |  |
| GENERALLY | Most moder- | Similar to | Animal and | Animal and |
| RESISTANT | ate chemi- | Natural Rub- | Vegetable | Vegetable |
| TO | cals, Wet of | ber | Oils, Greases, | Oils, Greases, |
|  | Dry, Organic |  | Ozones, | Ozones, |
|  | acids, Alco- |  | Strong and | Strong and |
|  | hols, Ketones, |  | Oxidizing | Oxidizing |
|  | Aldehydes |  | Chemicals | Chemicals |
| GENERALLY | Ozone, Strong | Similar to | Petroleum | Mineral Oils, |
| ATTACKED BY | Acids, Fats, | Natural Rub- | Solvents, Coal | and Solvents, |
|  | Oils, Greases, | ber | Tar Solvents, | Aromatic Hy- |
|  | Most Hydro- |  | Aromatic Hy- | drocarbons |
|  | carbons |  | drocarbons |  |

General Purpose - Oil Resistant

| (5) | (1) | (2) | (3) | (4) |
| --- | --- | --- | --- | --- |
| Nitrile | Epychlorohy- | Neoprene | Hypalon | Urethane |
|  | drin |  |  |  |
| NBR | CO | CR | CSM | AU |
|  | ECO |  |  | EU |
| Butadiene | Epichlo- | Chloroprene | Chloro- | Urethane |
| Acrylonitrile | rohydrin | Polymer | sulfonated | Polymer |
| Copolymer | Polymer and |  | Polyethylene |  |
|  | Copolymer |  |  |  |
| Many Hydro- | Similar to | Moderate | Similar to | ozone, |
| carbons, Fats, | Nitrile with | Chemicals | Neoprene with | hydrocarbons, |
| Oils, Greases, | Ozone Resis- | and Acids, | Improved Acid | moderate |
| Hydraulic | tance | Ozone, Oils, | Resistance | chemicals, |
| Fluids, Chemi- |  | Fats, Greases, |  | fats, |
| cals |  | Many Oils and |  |  |
|  |  | Solvents |  |  |
| Ozone * | Ketones, Esters, | Strong | Concentrated | Ozone, Hydro- |
| Ketones, Esters, | Aldehydes, | Oxidizing Acids, | Oxidizing Acids, | carbons, Moder- |
| Aldehydes, | Chlorinated and | Esters, Ketones, | Esters, Ketones, | ate Chemicals, |
| Chlorinated and | Hydrocarbons | Chlorinated, | Chlorinated, | Fats, |
| Nitro Hydrocar- |  | Aromatic, and | Aromatic, and |  |
| bons, *except |  | Hydrocarbons | Hydrocarbons |  |
| PVC Blends |  |  |  |  |

Specialty Elastomers

| fluid chart key | (10) | (11) | (12) | (13) | (14) |
| --- | --- | --- | --- | --- | --- |
| TYPE OF RUBBER | Polysulfide | Silicone | Fluoro | Fluoro | Poly |
|  |  |  | Silicone | Elastomer | Acrylate |
| Material and ASTM | T | Si | FSi | FPM | ACM |
| Designation |  |  |  |  |  |
| CHEMICAL GROUP | Organic Polysulfide | Organic Silicone Polymer | Fluorinated Organic | Fluorocarbon Polymer | Copolymer of Acrylic |
|  | Polymer |  | Silicone Polymer |  | Ester and Acrylic Halide |
| GENERALLY RESISTANT | Ozone, Oils, Solvents, | Moderate or Oxidiz- | Moderate or Oxidiz- | All Aliphatic, Aromatic, | Ozone, Extreme Pressure |
| TO | Thinners, Ketones, Esters, | ing Chemicals, Ozone, | ing Chemicals, Ozone, | and Halogenated Hydro- | Lubricants, Hot Oils, Pe- |
|  | Aromatic Hydrocarbons | Concentrated Sodium | Aromatic Chlorinated | carbons, Acids, Animal | troleum Solvents, Animal |
|  |  | Hydroxide | Solvents, Bases | and Vegetable Oils | and Vegetable Fats |
| GENERALLY ATTACKED | Mercaptans, Chlorinated | Many Solvents, Oils, Con- | Brake Fluids, Hydrazine | Ketones, Low Mole | Water, Alcohols, Glycols, |
| BY | Hydrocarbons, Nitro | centrated Acids, Dilute | Ketones | Weight Esters and Nitro | Alkali, Esters, Aromatic |
|  | Hydrocarbons, Ethers, | Sodium Hydroxide |  | Containing Compounds | Hydrocarbons, Halogenat- |
|  | Amines, Hetercocylics |  |  |  | ed Hydrocarbons Phenal |